ESSROC Materials Inc.

Southern Cement Division 1001 N. Hoskins Road Charlotte, NC   28216 704-393-9221

March 22, 1993

B. E. Kluttz Lbr. Co., Inc. 975 Davidson Drive NW Concord, NC 28025

ATTENTION:  Carolyn Kluttz

Fineness-Passing 1325 Sieve, Autoclave Expansion* X

ASTM C-91 Teat Report on Brixroent Masonry Cement-Type S

Typical

Test Results

97 .03

C-91 Requirements

76 Minimum 1i0

'hra. Minimum hra. Maximum

3 hra. 50 mine. 6 hre. 45 nins.

Time of Setting - Initial

Final

24

8-20

70 Minimum 110 +/- 5

17

83 111

Air Content* 2 Water Retention, % Original Flow of Mixture. Z Compraaaiva Strength, FSI

7-day* 28-daya

1,700 2.500

1,300 Minimum 2.100 Minimum

Thia la to certify that Brixroent-Type S Masonry Cement meeta the requirements of ASTM C-91 Standard Spacification for Masonry Cement Type S.

Sincerely,

James M. Porter Director of Sales Southeast Package

JMP:sw

Subscribed and sworn to before me this

22nd day of March, 1993,

NORATY PUBLIC

My Commission Expires 10'24-94